# Product description

Warm edge spacer Swisspacer Ultimate

Polymer SAN spacer with glass fibre (reinforced) content and high-tech gas barrier foil

Equivalent thermal conductivity (in accordance with ift guideline WA-17/1): λ = 0.14 W/mK

Available in a total of 17 RAL-like colours
RAL: 9023, 9005, 9016, 5003, 8003, 8014, 1016, 6018, 6026, 7013, 1011, 1034, 6010, 1015, 1001, 7035 or 8012

# Performance description

Can be used in multi-pane insulating glass units in accordance with DIN EN 1279

Example structures of multi-pane insulating glass units with Swisspacer Ultimate:

Double-sheet insulating glass (6 – 16 Ar – 6): Ug = 1.1 W/m²K

Triple-sheet insulating glass (6 – 12 Ar – 4 – 12 Ar – 6): Ug = 0.7 W/m²K

Physical values or Psi values (W/mK) for multi-pane insulating glass units with Swisspacer Ultimate depending on the façade profiles

Representative linear thermal conductivity coefficients (representative Psi values) as defined in ifa guideline WA-22/1 “Thermally improved spacers – Part 3: Determination of the representative Psi value for façade profiles”

Extract from datasheet Psi values façade profiles (May 2016 – No. CW19 – Revision index 4-06/2023 – valid until June 30th, 2025) © Arbeitskreis Warme Kante / BF Bundesverband Flachglas

# Product alternative

Warm edge spacer Swisspacer Advance

Polymer SAN spacer with glass fibre (reinforced) content and thermally improved aluminium foil

Equivalent thermal conductivity (in accordance with ift guideline WA-17/1): λ = 0.29 W/mK

Available in a total of 17 RAL-like colours
RAL 9023, 9005, 9016, 5003, 8003, 8014, 1016, 6018, 6026, 7013, 1011, 1034, 6010, 1015, 1001, 7035 or 8012

# Complementary product

Swisspacer Air for the permanent pressure equalisation of insulating glass units

The Swisspacer Air is a metal sleeve with an integrated special membrane. Swisspacer Air was developed as a permanent pressure equaliser in order to be able to transport multi-pane insulating glass units over differences in height and to minimize the distortions of the glass panes due to the climatic loads.

Technical Approval (DIBt) No. Z-70.4-249 of 11 March 2019 for: Pressure-equalising multi-pane insulating glass units with Swisspacer Air pressure relief valve

# Manufacturer

Swisspacer Vetrotech Saint-Gobain (International) AG
Zweigniederlassung Lengwil, Industriestrasse 8, 8574 Lengwil, Switzerland
www.swisspacer.com; info@swisspacer.com